HARDNESS CONVERSION TABLE (BASED ON BRINELL HARDNESS HB)

| Brinell | Brinell |  | Rockwell Hardness |  |  |  | Rockwell Superficial Hardness |  |  | Approximate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Indentation | 3000 kgf |  | Rockwell A | Rockwell B | Rockwell C | Rockwell D |  |  |  | Tensile |
| Diameter | 10 mm |  | 60 kgf | 100 kgf | 150 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Strength |
| mm | Ball | Vickers | Diamond | 1//16" ball | Diamond | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | ksi (MPa) |
|  | HB | HV | HRA | HRB | HRC | HRD | HR15N | HR30N | HR45N |  |
| --- | --- | 940 | 85.6 | --- | 68.0 | 76.9 | 93.2 | 84.4 | 75.4 | --- |
| --- | --- | 920 | 85.3 | --- | 67.5 | 76.5 | 93.0 | 84.0 | 74.8 | --- |
| --- | --- | 900 | 85.0 | --- | 67.0 | 76.1 | 92.9 | 83.6 | 74.2 | --- |
| --- | 767 | 880 | 84.7 | --- | 66.4 | 75.7 | 92.7 | 83.1 | 73.6 | --- |
| --- | 757 | 860 | 84.4 | --- | 65.9 | 75.3 | 92.5 | 82.7 | 73.1 | --- |
| 2.25 | 745 | 840 | 84.1 | --- | 65.3 | 74.8 | 92.3 | 82.2 | 72.2 | --- |
| --- | 733 | 820 | 83.8 | --- | 64.7 | 74.3 | 92.1 | 81.7 | 71.8 | --- |
| --- | 722 | 800 | 83.4 | --- | 64.0 | 73.8 | 91.8 | 81.1 | 71.0 | --- |
| 2.30 | 712 | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| --- | 710 | 780 | 83.0 | --- | 63.3 | 73.3 | 91.5 | 80.4 | 70.2 | --- |
| --- | 698 | 760 | 82.6 | --- | 62.5 | 72.6 | 91.2 | 79.7 | 69.4 | --- |
| --- | 684 | 740 | 82.2 | --- | 61.8 | 72.1 | 91.0 | 79.1 | 68. | --- |
| 2.35 | 682 | 737 | 82.2 | --- | 61.7 | 72.0 | 91.0 | 79.0 | 68.5 | --- |
| --- | 670 | 720 | 81.8 | --- | 61.0 | 71.5 | 90.7 | 78.4 | 67.7 | --- |
| --- | 656 | 700 | 81.3 | --- | 60.1 | 70.8 | 90.3 | 77.6 | 66.7 | --- |
| 2.40 | 653 | 697 | 81.2 | --- | 60.0 | 70.7 | 90.2 | 77.5 | 66.5 | --- |
| --- | 647 | 690 | 81.1 | --- | 59.7 | 70.5 | 90.1 | 77.2 | 66.2 | --- |
| --- | 638 | 680 | 80.8 | --- | 59.2 | 70.1 | 89.8 | 76.8 | 65.7 | --- |
| --- | 630 | 670 | 80.6 | --- | 58.8 | 69.8 | 89.7 | 76.4 | 65.3 | --- |
| 2.45 | 627 | 667 | 80.5 | --- | 58.7 | 69.7 | 89.6 | 76.3 | 65.1 | --- |
| 2.50 | --- 601 | 677 640 | 80.7 79.8 | --- --- | 59.1 57.3 | 70.0 68.7 | 89.8 89.0 | 76.8 75.1 | 65.7 63.5 | --- --- |
| Brinell | Brinell |  | Rockwell Hardness |  |  |  | Rockwell Superficial Hardness |  |  | Approximate |
| Indentation | 3000 kgf |  | Rockwell A | Rockwell B | Rockwell C | Rockwell D |  |  |  | Tensile |
| Diameter | 10 mm |  | 60 kgf | 100 kgf | 150 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Strength |
| mm | Ball | Vickers | Diamond | 1//16" ball | Diamond | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | ksi (MPa) |
|  | HB | HV | HRA | HRB | HRC | HRD | HR15N | HR30N | HR45N |  |
| 2.55 | --- 578 | 640 615 | 79.8 79.1 | --- --- | 57.3 56.0 | 68.7 67.7 | 89.0 88.4 | 75.1 73.9 | 63.5 62.1 | --- --- |
| 2.60 | --- 555 | 607 591 | 78.8 78.4 | --- --- | 55.6 54.7 | 67.4 66.7 | 88.1 87.8 | 73.5 72.7 | 61.6 60.6 | --- 2055 |
| 2.65 | --- 534 | 579 569 | 78.0 77.8 | --- --- | 54.0 53.5 | 66.1 65.8 | 87.5 87.2 | 72.0 71.6 | 59.8 59.2 | 2015 1985 |
| 2.70 | --- 514 | 553 547 | 77.1 76.9 | --- --- | 52.5 52.1 | 65.0 64.7 | 86.7 86.5 | 70.7 70.3 | 58.0 57.6 | 1915 1890 |
| 2.75 | --- --- 495 | 539 530 528 | 76.7 76.4 76.3 | --- --- --- | 51.6 51.1 51.0 | 64.3 63.9 63.8 | 86.3 86.0 85.9 | 69.9 69.5 69.4 | 56.9 56.2 56.1 | 1855 1825 1820 |
| 2.80 | --- 477 | 516 508 | 75.9 75.6 | --- --- | 50.3 49.6 | 63.2 62.7 | 85.6 85.3 | 68.7 68.2 | 55.2 54.5 | 1780 1740 |
| 2.85 | --- 461 | 495 491 | 75.1 74.9 | --- --- | 48.8 48.5 | 61.9 61.7 | 84.9 84.7 | 67.4 67.2 | 53.5 53.2 | 1680 1670 |
| 2.90 | --- 444 | 474 472 | 74.3 74.2 | --- --- | 47.2 47.1 | 61.0 60.8 | 84.1 84.0 | 66.0 65.8 | 51.7 51.5 | 1595 1585 |
| Brinell | Brinell |  | Rockwell Hardness |  |  |  | Rockwell Superficial Hardness |  |  | Approximate |
| Indentation | 3000 kgf |  | Rockwell A | Rockwell B | Rockwell C | Rockwell D |  |  |  | Tensile |
| Diameter | 10 mm |  | 60 kgf | 100 kgf | 150 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Strength |
| mm | Ball | Vickers | Diamond | 1//16" ball | Diamond | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | ksi (MPa) |
|  | HB | HV | HRA | HRB | HRC | HRD | HR15N | HR30N | HR45N |  |
| 2.95 | 429 | 455 | 73.4 | --- | 45.7 | 59.7 | 83.4 | 64.6 | 49.9 | 1510 |
| 3.00 | 415 | 440 | 72.8 | --- | 44.5 | 58.8 | 82.8 | 63.5 | 48.4 | 1460 |
| 3.05 | 401 | 425 | 72.0 | --- | 43.1 | 57.8 | 82.0 | 62.3 | 46.9 | 1390 |
| 3.10 | 388 | 410 | 71.4 | --- | 41.8 | 56.8 | 81.4 | 61.1 | 45.3 | 1330 |
| 3.15 | 375 | 396 | 70.6 | --- | 40.4 | 55.7 | 80.6 | 59.9 | 43.6 | 1270 |
| 3.20 | 363 | 383 | 70.0 | --- | 39.1 | 54.6 | 80.0 | 58.7 | 42.0 | 1220 |
| 3.25 | 352 | 372 | 69.3 | (110.0) | 37.9 | 53.8 | 79.3 | 57.6 | 40.5 | 1180 |
| 3.30 | 341 | 360 | 68.7 | (109.0) | 36.6 | 52.8 | 78.6 | 56.4 | 39.1 | 1130 |
| 3.35 | 331 | 350 | 68.1 | (108.5) | 35.5 | 51.9 | 78.0 | 55.4 | 37.8 | 1095 |
| 3.40 | 321 | 339 | 67.5 | (108.0) | 34.3 | 51.0 | 77.3 | 54.3 | 36.4 | 1060 |
| 3.45 | 311 | 328 | 66.9 | (107.5) | 33.1 | 50.0 | 76.7 | 53.3 | 34.4 | 1025 |
| 3.50 | 302 | 319 | 66.3 | (107.0) | 32.1 | 49.3 | 76.1 | 52.2 | 33.8 | 1005 |
| 3.55 | 293 | 309 | 65.7 | (106.0) | 30.9 | 48.3 | 75.5 | 51.2 | 32.4 | 970 |
| 3.60 | 285 | 301 | 65.3 | (105.5) | 29.9 | 47.6 | 75.0 | 50.3 | 31.2 | 950 |
| 3.65 | 277 | 292 | 64.6 | (104.5) | 28.8 | 46.7 | 74.4 | 49.3 | 29.9 | 925 |
| 3.70 | 269 | 284 | 64.1 | (104.0) | 27.6 | 45.9 | 73.7 | 48.3 | 28.5 | 895 |
| 3.75 | 262 | 276 | 63.6 | (103.0) | 26.6 | 45.0 | 73.1 | 47.3 | 27.3 | 875 |
| 3.80 | 255 | 269 | 63.0 | (102.0) | 25.4 | 44.2 | 72.5 | 46.2 | 26.0 | 850 |
| Brinell | Brinell |  | Rockwell Hardness |  |  |  | Rockwell Superficial Hardness |  |  | Approximate |
| Indentation | 3000 kgf |  | Rockwell A | Rockwell B | Rockwell C | Rockwell D |  |  |  | Tensile |
| Diameter | 10 mm |  | 60 kgf | 100 kgf | 150 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Strength |
| mm | Ball | Vickers | Diamond | 1//16" ball | Diamond | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | ksi (MPa) |
|  | HB | HV | HRA | HRB | HRC | HRD | HR15N | HR30N | HR45N |  |
| 3.85 | 248 | 261 | 62.5 | (101.0) | 24.2 | 43.2 | 71.7 | 45.1 | 24.5 | 825 |
| 3.90 | 241 | 253 | 61.8 | 100.0 | 22.8 | 42.0 | 70.9 | 43.9 | 22.8 | 800 |
| 3.95 | 235 | 247 | 61.4 | 99.0 | 21.7 | 41.4 | 70.3 | 42.9 | 21.5 | 785 |
| 4.00 | 229 | 241 | 60.8 | 98.2 | 20.5 | 40.5 | 69.7 | 41.9 | 20.1 | 765 |
| 4.05 | 223 | 234 |  | 97.3 | (18.8) | --- | --- | --- | --- | --- |
| 4.10 | 217 | 228 | --- | 96.4 | (17.5) | --- | --- | --- | --- | 725 |
| 4.15 | 212 | 222 | --- | 95.5 | (16.0) | --- | --- | --- | --- | 705 |
| 4.20 | 207 | 218 | --- | 94.6 | (15.2) | --- | --- | --- | --- | 690 |
| 4.25 | 201 | 212 | --- | 93.8 | (13.8) | --- | --- | --- | --- | 675 |
| 4.30 | 197 | 207 | --- | 92.8 | (12.7) | --- | --- | --- | --- | 655 |
| 4.35 | 192 | 202 | --- | 91.9 | (11.5) | --- | --- | --- | --- | 640 |
| 4.40 | 187 | 196 | --- | 90.7 | (10.0) | --- | --- | --- | --- | 620 |
| 4.45 | 183 | 192 | --- | 90.0 | (9.0) | --- | --- | --- | --- | 615 |
| 4.50 | 179 | 188 | --- | 89.0 | (8.0) | --- | --- | --- | --- | 600 |
| 4.55 | 174 | 182 | --- | 87.8 | (6.4) | --- | --- | --- | --- | 585 |
| 4.60 | 170 | 178 | --- | 86.8 | (5.4) | --- | --- | --- | --- | 570 |
| 4.65 | 167 | 175 | --- | 86.0 | (4.4) | --- | --- | --- | --- | 560 |
| 4.70 | 163 | 171 | --- | 85.0 | (3.3) | --- | --- | --- | --- | 545 |
| 4.80 | 156 | 163 | --- | 82.9 | (0.9) | --- | --- | --- | --- | 525 |
| 4.90 | 149 | 156 | --- | 80.8 | --- | --- | --- | --- | --- | 505 |
| Brinell | Brinell |  | Rockwell Hardness |  |  |  | Rockwell Superficial Hardness |  |  | Approximate |
| Indentation | 3000 kgf |  | Rockwell A | Rockwell B | Rockwell C | Rockwell D |  |  |  | Tensile |
| Diameter | 10 mm |  | 60 kgf | 100 kgf | 150 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Strength |
| mm | Ball | Vickers | Diamond | 1//16" ball | Diamond | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | ksi (MPa) |
|  | HB | HV | HRA | HRB | HRC | HRD | HR15N | HR30N | HR45N |  |
| 5.00 | 143 | 150 | --- | 78.7 | --- | --- | --- | --- | --- | 490 |
| 5.10 | 137 | 143 | --- | 76.4 | --- | --- | --- | --- | --- | 460 |
| 5.20 | 131 | 137 | --- | 74.0 | --- | --- | --- | --- | --- | 450 |
| 5.30 | 126 | 132 | --- | 72.0 | --- | --- | --- | --- | --- | 435 |
| 5.40 | 121 | 127 | --- | 69.8 | --- | --- | --- | --- | --- | 415 |
| 5.50 | 116 | 122 | --- | 67.6 | --- | --- | --- | --- | --- | 400 |
| 5.60 | 111 | 117 | --- | 65.7 | --- | --- | --- | --- | --- | 385 |

HARDNESS CONVERSION TABLE (BASED ON HRC)

|  |  | Brinell | Rockwell Hardness |  |  | Rockwell Superficial Hardness |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Rockwell C |  | 3000 kgf | Rockwell A | Rockwell B | Rockwell D |  |  |  | Approximate | Rockwell C |
| 150 kgf | Vickers | 10 mm | 60 kgf | 100 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Tensile | 150 kgf |
| Diamond | Hardness | Ball | Diamond | 1//16" ball | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | Strength | Diamond |
| HRC | HV | HB | HRA | HRB | HRD | HR15N | HR30N | HR45N | ksi (MPa) | HRC |
| 68 | 940 | --- | 85.6 | --- | 76.9 | 93.2 | 84.4 | 75.4 | --- | 68 |
| 67 | 900 | --- | 85.0 | --- | 76.1 | 92.9 | 83.6 | 74.2 | --- | 67 |
| 66 | 865 | --- | 84.5 | --- | 75.4 | 92.5 | 82.8 | 73.3 | --- | 66 |
| 65 | 832 | 739 | 83.9 | --- | 74.5 | 92.2 | 81.9 | 72.0 | --- | 65 |
| 64 | 800 | 722 | 83.4 | --- | 73.8 | 91.8 | 81.1 | 71.0 | --- | 64 |
| 63 | 772 | 705 | 82.8 | --- | 73.0 | 91.4 | 80.1 | 69.9 | --- | 63 |
| 62 | 746 | 688 | 82.3 | --- | 72.2 | 91.1 | 79.3 | 68.8 | --- | 62 |
| 61 | 720 | 670 | 81.8 | --- | 71.5 | 90.7 | 78.4 | 67.7 | --- | 61 |
| 60 | 697 | 654 | 81.2 | --- | 70.7 | 90.2 | 77.5 | 66.6 | --- | 60 |
| 59 | 674 | 634 | 80.7 | --- | 69.9 | 89.8 | 76.6 | 65.5 | --- | 59 |
| 58 | 653 | 615 | 80.1 | --- | 69.2 | 89.3 | 75.7 | 64.3 | --- | 58 |
| 57 | 633 | 595 | 79.6 | --- | 68.5 | 88.9 | 74.8 | 63.2 | --- | 57 |
| 56 | 613 | 577 | 79.0 | --- | 67.7 | 88.3 | 73.9 | 62.0 | --- | 56 |
| 55 | 595 | 560 | 78.5 | --- | 66.9 | 87.9 | 73.0 | 60.9 | 2075 | 55 |
| 54 | 577 | 543 | 78.0 | --- | 66.1 | 87.4 | 72.0 | 59.8 | 2015 | 54 |
| 53 | 560 | 525 | 77.4 | --- | 65.4 | 86.9 | 71.2 | 58.6 | 1950 | 53 |
| 52 | 544 | 512 | 76.8 | --- | 64.6 | 86.4 | 70.2 | 57.4 | 1880 | 52 |
| 51 | 528 | 496 | 76.3 | --- | 63.8 | 85.9 | 69.4 | 56.1 | 1820 | 51 |
| 50 | 513 | 481 | 75.9 | --- | 63.1 | 85.5 | 68.5 | 55.0 | 1760 | 50 |
| 49 | 498 | 469 | 75.2 | --- | 62.1 | 85.0 | 67.6 | 53.8 | 1695 | 49 |
|  |  | Brinell | Rockwell Hardness |  |  | Rockwell Superficial Hardness |  |  |  |  |
| Rockwell C |  | 3000 kgf | Rockwell A | Rockwell B | Rockwell D |  |  |  | Approximate | Rockwell C |
| 150 kgf | Vickers | 10 mm | 60 kgf | 100 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Tensile | 150 kgf |
| Diamond | Hardness | Ball | Diamond | 1//16" ball | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | Strength | Diamond |
| HRC | HV | HB | HRA | HRB | HRD | HR15N | HR30N | HR45N | ksi (MPa) | HRC |
| 48 | 484 | 455 | 74.7 | --- | 61.4 | 84.5 | 66.7 | 52.5 | 1635 | 48 |
| 47 | 471 | 443 | 74.1 | --- | 60.8 | 83.9 | 65.8 | 51.4 | 1580 | 47 |
| 46 | 458 | 432 | 73.6 | --- | 60.0 | 83.5 | 64.8 | 50.3 | 1530 | 46 |
| 45 | 446 | 421 | 73.1 | --- | 59.2 | 83.0 | 64.0 | 49.0 | 1480 | 45 |
| 44 | 434 | 409 | 72.5 | --- | 58.5 | 82.5 | 63.1 | 47.8 | 1435 | 44 |
| 43 | 423 | 400 | 72.0 | --- | 57.7 | 82.0 | 62.2 | 46.7 | 1385 | 43 |
| 42 | 412 | 390 | 71.5 | --- | 56.9 | 81.5 | 61.3 | 45.5 | 1340 | 42 |
| 41 | 402 | 381 | 70.9 | --- | 56.2 | 80.9 | 60.4 | 44.3 | 1295 | 41 |
| 40 | 392 | 371 | 70.4 | --- | 55.4 | 80.4 | 59.5 | 43.1 | 1250 | 40 |
| 39 | 382 | 362 | 69.9 | --- | 54.6 | 79.9 | 58.6 | 41.9 | 1215 | 39 |
| 38 | 372 | 353 | 69.4 | --- | 53.8 | 79.4 | 57.7 | 40.8 | 1180 | 38 |
| 37 | 363 | 344 | 68.9 | --- | 53.1 | 78.8 | 56.8 | 39.6 | 1160 | 37 |
| 36 | 354 | 336 | 68.4 | (109.0) | 52.3 | 78.3 | 55.9 | 38.4 | 1115 | 36 |
| 35 | 345 | 327 | 67.9 | (108.5) | 51,5 | 77.7 | 55.0 | 37.2 | 1080 | 35 |
| 34 | 336 | 319 | 67.4 | (108.0) | 50.8 | 77.2 | 54.2 | 36.1 | 1055 | 34 |
| 33 | 327 | 311 | 66.8 | (107.5) | 50.0 | 76.6 | 53.3 | 34.9 | 1025 | 33 |
| 32 | 318 | 301 | 66.3 | (107.0) | 49.2 | 76.1 | 52.1 | 33.7 | 1000 | 32 |
| 31 | 310 | 294 | 65.8 | (106.0) | 48.4 | 75.6 | 51.3 | 32.5 | 980 | 31 |
| 30 | 302 | 286 | 65.3 | (105.5) | 47.7 | 75.0 | 50.4 | 31.3 | 950 | 30 |
| 29 | 294 | 279 | 64.7 | (104.5) | 47.0 | 74.5 | 49.5 | 30.1 | 930 | 29 |
|  |  | Brinell | Rockwell Hardness |  |  | Rockwell Superficial Hardness |  |  |  |  |
| Rockwell C | 286 | 3000 kgf | Rockwell A | Rockwell B | Rockwell D |  |  |  | Approximate | Rockwell C |
| 150 kgf | Vicke279rs | 10 mm | 60 kgf | 100 kgf | 100 kgf | 15 kgf | 30 kgf | 45 kgf | Tensile | 150 kgf |
| Diamond | Hardnes272s | Ball | Diamond | 1//16" ball | Diamond | 1/16" ball | 1/16" ball | 1/16" ball | Strength | Diamond |
| HRC | HV | HB | HRA | HRB | HRD | HR15N | HR30N | HR45N | ksi (MPa) | HRC |
| 28 | 286 | 271 | 64.3 | (104.0) | 46.1 | 73.9 | 48.6 | 28.9 | 910 | 28 |
| 27 | 279 | 264 | 63.8 | (103.0) | 45.2 | 73.3 | 47.7 | 27.8 | 880 | 27 |
| 26 | 272 | 258 | 63.3 | (102.5) | 44.6 | 72.8 | 46.8 | 26.7 | 860 | 26 |
| 25 | 266 | 253 | 62.8 | (101.5) | 43.8 | 72.2 | 45.9 | 25.5 | 840 | 25 |
| 24 | 260 | 247 | 62.4 | (101.0) | 43.1 | 71.6 | 45.0 | 24.3 | 825 | 24 |
| 23 | 254 | 243 | 62.0 | 100.0 | 42.1 | 71.0 | 44.0 | 23.1 | 805 | 23 |
| 22 | 248 | 237 | 61.5 | 99.0 | 41.6 | 70.5 | 43.2 | 22.0 | 785 | 22 |
| 21 | 243 | 231 | 61.0 | 98.5 | 40.9 | 69.9 | 42.3 | 20.7 | 770 | 21 |
| 20 | 238 | 226 | 60.5 | 97.8 | 40.1 | 69.4 | 41.5 | 19.6 | 760 | 20 |
| (18) | 230 | 219 | --- | 96.7 | --- | --- | --- | --- | 730 | (18) |
| (16) | 222 | 212 | --- | 95.5 | --- | --- | --- | --- | 705 | (16) |
| (14) | 213 | 203 | --- | 93.9 | --- | --- | --- | --- | 675 | (14) |
| (12) | 204 | 194 | --- | 92.3 | --- | --- | --- | --- | 650 | (12) |
| (10) | 196 | 187 | --- | 90.7 | --- | --- | --- | --- | 620 | (10) |
| (8) | 188 | 179 | --- | 89.5 | --- | --- | --- | --- | 600 | (8) |
|  |  |  |  |  |  |  |  | --- |  |  |
| (6) | 180 | 171 | --- | 87.1 | --- | --- | --- | --- | 580 | (6) |
| (4) | 173 | 165 | --- | 85.5 | --- | --- | --- | --- | 550 | (4) |
| (2) | 166 | 158 | --- | 83.5 | --- | --- | --- | --- | 530 | (2) |
| (0) | 160 | 152 | --- | 81.7 | --- | --- | --- | --- | 510 | (0) |

# ASTM E 140 Hardness Conversion Tables for Metals

## ASTM E140 Standard Hardness Conversion Tables for Metals-Relationship Among Brinell Hardness, Vickers Hardness, Rockwell Hardness, Knoop Hardness, Superficial Hardness, and Scleroscope Hardness

#### Approximate Hardness Conversion Numbers for Non-Austenitic Steels (Rockwell C Hardness Range) A, B

| Rockwell C Hardness Number 150 kgf (HRC) | Vickers Hardness Number (HV) | Brinell Hardness Number C |  | Knoop Hardness, Number 500-gf and Over (HK) | Rockwell Hardness Number |  | Rockwell Superficial Hardness Number |  |  | Scleroscope Hardness Number D | Rockwell C Hardness Number 150 kgf (HRC) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 10-mm Standard Ball, 3000-kgf (HBS) | 10-mm Carbide Ball, 3000-kgf (HBW) |  | A Scale, 60-kgf (HRA) | D Scale, 100-kgf (HRD) | 15-N Scale, 15-kgf (HR 15-N) | 30-N Scale, 30-kgf (HR 30-N) | 45-N Scale, 45-kgf (HR 45-N) |  |  |
| 68 | 940 | --- | --- | 920 | 85.6 | 76.9 | 93.2 | 84.4 | 75.4 | 97.3 | 68 |
| 67 | 900 | --- | --- | 895 | 85.0 | 76.1 | 92.9 | 83.6 | 74.2 | 95.0 | 67 |
| 66 | 865 | --- | --- | 870 | 84.5 | 75.4 | 92.5 | 82.8 | 73.3 | 92.7 | 66 |
| 65 | 832 | --- | (739) | 846 | 83.9 | 74.5 | 92.2 | 81.9 | 72.0 | 90.6 | 65 |
| 64 | 800 | --- | (722) | 822 | 83.4 | 73.8 | 91.8 | 81.1 | 71.0 | 88.5 | 64 |
| 63 | 772 | --- | (705) | 799 | 82.8 | 73.0 | 91.4 | 80.1 | 69.9 | 86.5 | 63 |
| 62 | 746 | --- | (688) | 776 | 82.3 | 72.2 | 91.1 | 79.3 | 68.8 | 84.5 | 62 |
| 61 | 720 | --- | (670) | 754 | 81.8 | 71.5 | 90.7 | 78.4 | 67.7 | 82.6 | 61 |
| 60 | 697 | --- | (654) | 732 | 81.2 | 70.7 | 90.2 | 77.5 | 66.6 | 80.8 | 60 |
| 59 | 674 | --- | 634 | 710 | 80.7 | 69.9 | 89.8 | 76.6 | 65.5 | 79.0 | 59 |
| 58 | 653 | --- | 615 | 690 | 80.1 | 69.2 | 89.3 | 75.7 | 64.3 | 77.3 | 58 |
| 57 | 633 | --- | 595 | 670 | 79.6 | 68.5 | 88.9 | 74.8 | 63.2 | 75.6 | 57 |
| 56 | 613 | --- | 577 | 650 | 79.0 | 67.7 | 88.3 | 73.9 | 62.0 | 74.0 | 56 |
| 55 | 595 | --- | 560 | 630 | 78.5 | 66.9 | 87.9 | 73.0 | 60.9 | 72.4 | 55 |
| 54 | 577 | --- | 543 | 612 | 78.0 | 66.1 | 87.4 | 72.0 | 59.8 | 70.9 | 54 |
| 53 | 560 | --- | 525 | 594 | 77.4 | 65.4 | 86.9 | 71.2 | 58.6 | 69.4 | 53 |
| 52 | 544 | (500) | 512 | 576 | 76.8 | 64.6 | 86.4 | 70.2 | 57.4 | 67.9 | 52 |
| 51 | 528 | (487) | 496 | 558 | 76.3 | 63.8 | 85.9 | 69.4 | 56.1 | 66.5 | 51 |
| 50 | 513 | (475) | 481 | 542 | 75.9 | 63.1 | 85.5 | 68.5 | 55.0 | 65.1 | 50 |
| 49 | 498 | (464) | 469 | 526 | 75.2 | 62.1 | 85.0 | 67.6 | 53.8 | 63.7 | 49 |
| 48 | 484 | 451 | 455 | 510 | 74.7 | 61.4 | 84.5 | 66.7 | 52.5 | 62.4 | 48 |
| 47 | 471 | 442 | 443 | 495 | 74.1 | 60.8 | 83.9 | 65.8 | 51.4 | 61.1 | 47 |
| 46 | 458 | 432 | 432 | 480 | 73.6 | 60.0 | 83.5 | 64.8 | 50.3 | 59.8 | 46 |
| Rockwell C Hardness Number 150 kgf (HRC) | Vickers Hardness Number (HV) | Brinell Hardness Number C |  | Knoop Hardness, Number 500-gf and Over (HK) | Rockwell Hardness Number |  | Rockwell Superficial Hardness Number |  |  | Scleroscope Hardness Number D | Rockwell C Hardness Number 150 kgf (HRC) |
|  |  | 10-mm Standard Ball, 3000-kgf (HBS) | 10-mm Carbide Ball, 3000-kgf (HBW) |  | A Scale, 60-kgf (HRA) | D Scale, 100-kgf (HRD) | 15-N Scale, 15-kgf (HR 15-N) | 30-N Scale, 30-kgf (HR 30-N) | 45-N Scale, 45-kgf (HR 45-N) |  |  |
| 45 | 446 | 421 | 421 | 466 | 73.1 | 59.2 | 83.0 | 64.0 | 49.0 | 58.5 | 45 |
| 44 | 434 | 409 | 409 | 452 | 72.5 | 58.5 | 82.5 | 63.1 | 47.8 | 57.3 | 44 |
| 43 | 423 | 400 | 400 | 438 | 72.0 | 57.7 | 82.0 | 62.2 | 46.7 | 56.1 | 43 |
| 42 | 412 | 390 | 390 | 426 | 71.5 | 56.9 | 81.5 | 61.3 | 45.5 | 54.9 | 42 |
| 41 | 402 | 381 | 381 | 414 | 70.9 | 56.2 | 80.9 | 60.4 | 44.3 | 53.7 | 41 |
| 40 | 392 | 371 | 371 | 402 | 70.4 | 55.4 | 80.4 | 59.5 | 43.1 | 52.6 | 40 |
| 39 | 382 | 362 | 362 | 391 | 69.9 | 54.6 | 79.9 | 58.6 | 41.9 | 51.5 | 39 |
| 38 | 372 | 353 | 353 | 380 | 69.4 | 53.8 | 79.4 | 57.7 | 40.8 | 50.4 | 38 |
| 37 | 363 | 344 | 344 | 370 | 68.9 | 53.1 | 78.8 | 56.8 | 39.6 | 49.3 | 37 |
| 36 | 354 | 336 | 336 | 360 | 68.4 | 52.3 | 78.3 | 55.9 | 38.4 | 48.2 | 36 |
| 35 | 345 | 327 | 327 | 351 | 67.9 | 51.5 | 77.7 | 55.0 | 37.2 | 47.1 | 35 |
| 34 | 336 | 319 | 319 | 342 | 67.4 | 50.8 | 77.2 | 54.2 | 36.1 | 46.1 | 34 |
| 33 | 327 | 311 | 311 | 334 | 66.8 | 50.0 | 76.6 | 53.3 | 34.9 | 45.1 | 33 |
| 32 | 318 | 301 | 301 | 326 | 66.3 | 49.2 | 76.1 | 52.1 | 33.7 | 44.1 | 32 |
| 31 | 310 | 294 | 294 | 318 | 65.8 | 48.4 | 75.6 | 51.3 | 32.5 | 43.1 | 31 |
| 30 | 302 | 286 | 286 | 311 | 65.3 | 47.7 | 75.0 | 50.4 | 31.3 | 42.2 | 30 |
| 29 | 294 | 279 | 279 | 304 | 64.8 | 47.0 | 74.5 | 49.5 | 30.1 | 41.3 | 29 |
| 28 | 286 | 271 | 271 | 297 | 64.3 | 46.1 | 73.9 | 48.6 | 28.9 | 40.4 | 28 |
| 27 | 279 | 264 | 264 | 290 | 63.8 | 45.2 | 73.3 | 47.7 | 27.8 | 39.5 | 27 |
| 26 | 272 | 258 | 258 | 284 | 63.3 | 44.6 | 72.8 | 46.8 | 26.7 | 38.7 | 26 |
| 25 | 266 | 253 | 253 | 278 | 62.8 | 43.8 | 72.2 | 45.9 | 25.5 | 37.8 | 25 |
| 24 | 260 | 247 | 247 | 272 | 62.4 | 43.1 | 71.6 | 45.0 | 24.3 | 37.0 | 24 |
| 23 | 254 | 243 | 243 | 266 | 62.0 | 42.1 | 71.0 | 44.0 | 23.1 | 36.3 | 23 |
| 22 | 248 | 237 | 237 | 261 | 61.5 | 41.6 | 70.5 | 43.2 | 22.0 | 35.5 | 22 |
| 21 | 243 | 231 | 231 | 256 | 61.0 | 40.9 | 69.9 | 42.3 | 20.7 | 34.8 | 21 |
| 20 | 238 | 226 | 226 | 251 | 60.5 | 40.1 | 69.4 | 41.5 | 19.6 | 34.2 | 20 |
| A In the table headings, force refers to total test forces. B Appendix X1 contains equations converting determined hardness scale numbers to Rockwell C hardness numbers for non-austenitic steels. C The Brinell hardness numbers in parentheses are outside the range recommended for Brinell hardness testing in 8.1 of Test Method E 10. D These Scleroscope hardness conversions are based on Vickers—Scleroscope hardness relationships developed from Vickers hardness data provided by the National Bureau of Standards for 13 steel reference blocks, Scleroscope hardness values obtained on these blocks by the Shore Instrument and Mfg. Co., Inc., the Roll Manufacturers Institute, and members of this institute, and also on hardness conversions previously published by the American Society for Metals and the Roll Manufacturers Institute. |  |  |  |  |  |  |  |  |  |  |  |

#### Approximate Hardness Conversion Numbers for Non-Austenitic Steels (Rockwell B Hardness Range) A, B

| Rockwell B Hardness Number, 100-kgf (HRB) | Vickers Hardness Number (HV) | Brinell Hardness Number, 3000-kgf, (HBS) | Knoop Hardness Number, 500-gf, and Over (HK) | Rockwell A Hardness Number, 60-kgf, (HRA) | Rockwell F Hardness Number, 60-kgf, (HRF) | Rockwell Superficial Hardness Number |  |  | Rockwell B Hardness Number, 100-kgf, (HRB) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | 15-T Scale, 15-kgf, (HR 15-T) | 30-T Scale, 30-kgf, (HR 30-T) | 45-T Scale, 45-kgf, (HR 45-T) |  |
| 100 | 240 | 240 | 251 | 61.5 | --- | 93.1 | 83.1 | 72.9 | 100 |
| 99 | 234 | 234 | 246 | 60.9 | --- | 92.8 | 82.5 | 71.9 | 99 |
| 98 | 228 | 228 | 241 | 60.2 | --- | 92.5 | 81.8 | 70.9 | 98 |
| 97 | 222 | 222 | 236 | 59.5 | --- | 92.1 | 81.1 | 69.9 | 97 |
| 96 | 216 | 216 | 231 | 58.9 | --- | 91.8 | 80.4 | 68.9 | 96 |
| 95 | 210 | 210 | 226 | 58.3 | --- | 91.5 | 79.8 | 67.9 | 95 |
| 94 | 205 | 205 | 221 | 57.6 | --- | 91.2 | 79.1 | 66.9 | 94 |
| 93 | 200 | 200 | 216 | 57.0 | --- | 90.8 | 78.4 | 65.9 | 93 |
| 92 | 195 | 195 | 211 | 56.4 | --- | 90.5 | 77.8 | 64.8 | 92 |
| 91 | 190 | 190 | 206 | 55.8 | --- | 90.2 | 77.1 | 63.8 | 91 |
| 90 | 185 | 185 | 201 | 55.2 | --- | 89.9 | 76.4 | 62.8 | 90 |
| 89 | 180 | 180 | 196 | 54.6 | --- | 89.5 | 75.8 | 61.8 | 89 |
| 88 | 176 | 176 | 192 | 54.0 | --- | 89.2 | 75.1 | 60.8 | 88 |
| 87 | 172 | 172 | 188 | 53.4 | --- | 88.9 | 74.4 | 59.8 | 87 |
| 86 | 169 | 169 | 184 | 52.8 | --- | 88.6 | 73.8 | 58.8 | 86 |
| 85 | 165 | 165 | 180 | 52.3 | --- | 88.2 | 73.1 | 57.8 | 85 |
| 84 | 162 | 162 | 176 | 51.7 | --- | 87.9 | 72.4 | 56.8 | 84 |
| 83 | 159 | 159 | 173 | 51.1 | --- | 87.6 | 71.8 | 55.8 | 83 |
| 82 | 156 | 156 | 170 | 50.6 | --- | 87.3 | 71.1 | 54.8 | 82 |
| 81 | 153 | 153 | 167 | 50.0 | --- | 86.9 | 70.4 | 53.8 | 81 |
| 80 | 150 | 150 | 164 | 49.5 | --- | 86.6 | 69.7 | 52.8 | 80 |
| 79 | 147 | 147 | 161 | 48.9 | --- | 86.3 | 69.1 | 51.8 | 79 |
| Rockwell B Hardness Number, 100-kgf (HRB) | Vickers Hardness Number (HV) | Brinell Hardness Number, 3000-kgf, (HBS) | Knoop Hardness Number, 500-gf, and Over (HK) | Rockwell A Hardness Number, 60-kgf, (HRA) | Rockwell F Hardness Number, 60-kgf, (HRF) | Rockwell Superficial Hardness Number |  |  | Rockwell B Hardness Number, 100-kgf, (HRB) |
|  |  |  |  |  |  | 15-T Scale, 15-kgf, (HR 15-T) | 30-T Scale, 30-kgf, (HR 30-T) | 45-T Scale, 45-kgf, (HR 45-T) |  |
| 78 | 144 | 144 | 158 | 48.4 | --- | 86.0 | 68.4 | 50.8 | 78 |
| 77 | 141 | 141 | 155 | 47.9 | --- | 85.6 | 67.7 | 49.8 | 77 |
| 76 | 139 | 139 | 152 | 47.3 | --- | 85.3 | 67.1 | 48.8 | 76 |
| 75 | 137 | 137 | 150 | 46.8 | 99.6 | 85.0 | 66.4 | 47.8 | 75 |
| 74 | 135 | 135 | 147 | 46.3 | 99.1 | 84.7 | 65.7 | 46.8 | 74 |
| 73 | 132 | 132 | 145 | 45.8 | 98.5 | 84.3 | 65.1 | 45.8 | 73 |
| 72 | 130 | 130 | 143 | 45.3 | 98.0 | 84.0 | 64.4 | 44.8 | 72 |
| 71 | 127 | 127 | 141 | 44.8 | 97.4 | 83.7 | 63.7 | 43.8 | 71 |
| 70 | 125 | 125 | 139 | 44.3 | 96.8 | 83.4 | 63.1 | 42.8 | 70 |
| 69 | 123 | 123 | 137 | 43.8 | 96.2 | 83.0 | 62.4 | 41.8 | 69 |
| 68 | 121 | 121 | 135 | 43.3 | 95.6 | 82.7 | 61.7 | 40.8 | 68 |
| 67 | 119 | 119 | 133 | 42.8 | 95.1 | 82.4 | 61.0 | 39.8 | 67 |
| 66 | 117 | 117 | 131 | 42.3 | 94.5 | 82.1 | 60.4 | 38.7 | 66 |
| 65 | 116 | 116 | 129 | 41.8 | 93.9 | 81.8 | 59.7 | 37.7 | 65 |
| 64 | 114 | 114 | 127 | 41.4 | 93.4 | 81.4 | 59.0 | 36.7 | 64 |
| 63 | 112 | 112 | 125 | 40.9 | 92.8 | 81.1 | 58.4 | 35.7 | 63 |
| 62 | 110 | 110 | 124 | 40.4 | 92.2 | 80.8 | 57.7 | 34.7 | 62 |
| 61 | 108 | 108 | 122 | 40.0 | 91.7 | 80.5 | 57.0 | 33.7 | 61 |
| 60 | 107 | 107 | 120 | 39.5 | 91.1 | 80.1 | 56.4 | 32.7 | 60 |
| 59 | 106 | 106 | 118 | 39.0 | 90.5 | 79.8 | 55.7 | 31.7 | 59 |
| 58 | 104 | 104 | 117 | 38.6 | 90.0 | 79.5 | 55.0 | 30.7 | 58 |
| 57 | 103 | 103 | 115 | 38.1 | 89.4 | 79.2 | 54.4 | 29.7 | 57 |
| 56 | 101 | 101 | 114 | 37.7 | 88.8 | 78.8 | 53.7 | 28.7 | 56 |
| 55 | 100 | 100 | 112 | 37.2 | 88.2 | 78.5 | 53.0 | 27.7 | 55 |
| 54 | --- | --- | 111 | 36.8 | 87.7 | 78.2 | 52.4 | 26.7 | 54 |
| Rockwell B Hardness Number, 100-kgf (HRB) | Vickers Hardness Number (HV) | Brinell Hardness Number, 3000-kgf, (HBS) | Knoop Hardness Number, 500-gf, and Over (HK) | Rockwell A Hardness Number, 60-kgf, (HRA) | Rockwell F Hardness Number, 60-kgf, (HRF) | Rockwell Superficial Hardness Number |  |  | Rockwell B Hardness Number, 100-kgf, (HRB) |
|  |  |  |  |  |  | 15-T Scale, 15-kgf, (HR 15-T) | 30-T Scale, 30-kgf, (HR 30-T) | 45-T Scale, 45-kgf, (HR 45-T) |  |
| 53 | --- | --- | 110 | 36.3 | 87.1 | 77.9 | 51.7 | 25.7 | 53 |
| 52 | --- | --- | 109 | 35.9 | 86.5 | 77.5 | 51.0 | 24.7 | 52 |
| 51 | --- | --- | 108 | 35.5 | 86.0 | 77.2 | 50.3 | 23.7 | 51 |
| 50 | --- | --- | 107 | 35.0 | 85.4 | 76.9 | 49.7 | 22.7 | 50 |
| 49 | --- | --- | 106 | 34.6 | 84.8 | 76.6 | 49.0 | 21.7 | 49 |
| 48 | --- | --- | 105 | 34.1 | 84.3 | 76.2 | 48.3 | 20.7 | 48 |
| 47 | --- | --- | 104 | 33.7 | 83.7 | 75.9 | 47.7 | 19.7 | 47 |
| 46 | --- | --- | 103 | 33.3 | 83.1 | 75.6 | 47.0 | 18.7 | 46 |
| 45 | --- | --- | 102 | 32.9 | 82.6 | 75.3 | 46.3 | 17.7 | 45 |
| 44 | --- | --- | 101 | 32.4 | 82.0 | 74.9 | 45.7 | 16.7 | 44 |
| 43 | --- | --- | 100 | 32.0 | 81.4 | 74.6 | 45.0 | 15.7 | 43 |
| 42 | --- | --- | 99 | 31.6 | 80.8 | 74.3 | 44.3 | 14.7 | 42 |
| 41 | --- | --- | 98 | 31.2 | 80.3 | 74.0 | 43.7 | 13.6 | 41 |
| 40 | --- | --- | 97 | 30.7 | 79.7 | 73.6 | 43.0 | 12.6 | 40 |
| 39 | --- | --- | 96 | 30.3 | 79.1 | 73.3 | 42.3 | 11.6 | 39 |
| 38 | --- | --- | 95 | 29.9 | 78.6 | 73.0 | 41.6 | 10.6 | 38 |
| 37 | --- | --- | 94 | 29.5 | 78.0 | 72.7 | 41.0 | 9.6 | 37 |
| 36 | --- | --- | 93 | 29.1 | 77.4 | 72.3 | 40.3 | 8.6 | 36 |
| 35 | --- | --- | 92 | 28.7 | 76.9 | 72.0 | 39.6 | 7.6 | 35 |
| 34 | --- | --- | 91 | 28.2 | 76.3 | 71.7 | 39.0 | 6.6 | 34 |
| 33 | --- | --- | 90 | 27.8 | 75.7 | 71.4 | 38.3 | 5.6 | 33 |
| 32 | --- | --- | 89 | 27.4 | 75.2 | 71.0 | 37.6 | 4.6 | 32 |
| 31 | --- | --- | 88 | 27.0 | 74.6 | 70.7 | 37.0 | 3.6 | 31 |
| 30 | --- | --- | 87 | 26.6 | 74.0 | 70.4 | 36.3 | 2.6 | 30 |
| A In table headings, kgf refers to total test force. B Appendix X2 contains equations converting determined hardness numbers to Rockwell B hardness numbers for non-austenitic steels. Refer to 1.11 before using conversion equations. |  |  |  |  |  |  |  |  |  |

#### Approximate Hardness Conversion Numbers for Non-Austenitic Steels (Rockwell C Hardness Range) Rockwell Hardness Number, B Scale (100-kgf, 1⁄16-in. (1.588-mm) ball) (HRB); Brinell Hardness Number (3000-kgf, 10-mm ball) (HBS). 100; 256. 99; 248. 98; 240. 97; 233. 96; 226. 95; 219. 94; 213. 93; 207. 92; 202. 91; 197. 90; 192. 89; 187. 88; 183. 87; 178. 86; 174. 85; 170. 84; 167. 83; 163. 82; 160. 81; 156. 80; 153. 79; 150. 78; 147. 77; 144. 76; 142. 75; 139. 74; 137. 73; 135. 72; 132. 71; 130. 70; 128. 69; 126. 68; 124. 67; 122. 66; 120. 65; 118. 64; 116. 63; 114. 62; 113. 61; 111. 60; 110. #### Approximate Rockwell Hardness Conversion Numbers for Austenitic Stainless Steel Sheet A,B Rockwell Hardness Number; Rockwell Superficial Hardness Number. C Scale, 150-kgf Diamond Penetrator (HRC); A Scale, 60-kgf, Diamond Penetrator (HRA); 15-N Scale, 15-kgf, Superficial Diamond Penetrator (HR 15-N); 30-N Scale, 30-kgf, Superficial Diamond Penetrator (HR 30-N); 45-N Scale, 45-kgf, Superficial Diamond Penetrator (HR 45-N). 48; 74.4; 84.1; 66.2; 52.1. 47; 73.9; 83.6; 65.3; 50.9. 46; 73.4; 83.1; 64.5; 49.8. 45; 72.9; 82.6; 63.6; 48.7. 44; 72.4; 82.1; 62.7; 47.5. 43; 71.9; 81.6; 61.8; 46.4. 42; 71.4; 81.0; 61.0; 45.2. 41; 70.9; 80.5; 60.1; 44.1. 40; 70.4; 80.0; 59.2; 43.0. 39; 69.9; 79.5; 58.4; 41.8. 38; 69.3; 79.0; 57.5; 40.7. 37; 68.8; 78.5; 56.6; 39.6. 36; 68.3; 78; 55.7; 38.4. 35; 67.8; 77.5; 54.9; 37.3. 34; 67.3; 77.0; 54.0; 36.1. 33; 66.8; 76.5; 53.1; 35.0. 32; 66.3; 75.9; 52.3; 33.9. 31; 65.8; 75.4; 51.4; 32.7. 30; 65.3; 74.9; 50.5; 31.6. 29; 64.8; 74.4; 49.6; 30.4. 28; 64.3; 73.9; 48.8; 29.3. 27; 63.8; 73.4; 47.9; 28.2. 26; 63.3; 72.9; 47.0; 27.0. 25; 62.8; 72.4; 46.2; 25.9. 24; 62.3; 71.9; 45.3; 24.8. 23; 61.8; 71.3; 44.4; 23.6. 22; 61.3; 70.8; 43.5; 22.5. 21; 60.8; 70.3; 42.7; 21.3. 20; 60.3; 69.8; 41.8; 20.2. B Scale, 100-kgf, 1/16-in. (1.588-mm) Ball (HRB); A Scale, 60-kgf, Diamond Penetrator (HRA); F Scale, 60-kgf, 1/16-in. (1.588-mm) Ball C (HRF); 15-T Scale, 15-kgf, 1/16-in. (1.588-mm) Ball (HR 15-T); 30-T Scale, 30-kgf, 1/16-in. (1.588-mm) Ball (HR 30-T); 45-T Scale, 45-kgf, 1/16-in. (1.588-mm) Ball (HR 45-T). 100. 99. 98. 97. 96. 95. 94. 93. 92. 91. 90. 89. 88. 87. 86. 85. 84. 83. 82. 81. 80. 79. 78. 77. 76. 75. 74. 73. 72. 71. 70. 69. 68. 67. 66. 65. 64. 63. 62. 61. 60. Standard deviation C.; 61.5. 60.9. 60.3. 59.7. 59.1. 58.5. 58.0. 57.4. 56.8. 56.2. 55.6. 55.0. 54.5. 53.9. 53.3. 52.7. 52.1. 51.5. 50.9. 50.4. 49.8. 49.2. 48.6. 48.0. 47.4. 46.9. 46.3. 45.7. 45.1. 44.5. 43.9. 43.3. 42.8. 42.2. 41.6. 41.0. 40.4. 39.8. 39.3. 38.7. 38.1. 1.44.; (113.9). (113.2). (112.5). (111.8). (111.1). (110.5). (109.8). (109.1). (108.4). (107.8). (107.1). (106.4). (105.7). (105.0). (104.4). (103.7). (103.0). (102.3). (101.7). (101.0). (100.3). 99.6. 99.0. 98.3. 97.6. 96.9. 96.2. 95.6. 94.9. 94.2. 93.5. 92.8. 92.2. 91.5. 90.8. 90.1. 89.5. 88.8. 88.1. 87.4. 86.8. 2.75.; 91.5. 91.2. 90.8. 90.4. 90.1. 89.7. 89.3. 88.9. 88.6. 88.2. 87.8. 87.5. 87.1. 86.7. 86.4. 86.0. 85.6. 85.2. 84.9. 84.5. 84.1. 83.8. 83.4. 83.0. 82.6. 82.3. 81.9. 81.5. 81.2. 80.8. 80.4. 80.1. 79.7. 79.3. 78.9. 78.6. 78.2. 77.8. 77.5. 77.1. 76.7. 2.29.; 80.4. 79.7. 79.0. 78.3. 77.7. 77.0. 76.3. 75.6. 74.9. 74.2. 73.5. 72.8. 72.1. 71.4. 70.7. 70.0. 69.3. 68.6. 67.9. 67.2. 66.5. 65.8. 65.1. 64.4. 63.7. 63.0. 62.4. 61.7. 61.0. 60.3. 59.6. 58.9. 58.2. 57.5. 56.8. 56.1. 55.4. 54.7. 54.0. 53.3. 52.6. 1.67.; 70.2. 69.2. 68.2. 67.2. 66.1. 65.1. 64.1. 63.1. 62.1. 61.1. 60.1. 59.0. 58.0. 57.0. 56.0. 55.0. 54.0. 52.9. 51.9. 50.9. 49.9. 48.9. 47.9. 46.8. 45.8. 44.8. 43.8. 42.8. 41.8. 40.7. 39.7. 38.7. 37.7. 36.7. 35.7. 34.7. 33.6. 32.6. 31.6. 30.6. 29.6. 1.57... A In table headings, kgf or gf refers to total test force. B Appendix X6 contains equations converting determined hardness numbers to Rockwell C and Rockwell B hardness numbers for austenitic stainless steel sheet. Refer to 1.11 before using conversion equations. C Observed standard deviation of the inter-laboratory test data about the indicated conversion line..