### Modulus of Rigidity of some Common Materials

### The rigidity is found from the slope of the stress/strain curve of a material under tensile stress tests.  The modulus of rigidity is the coefficient of elasticity for a shearing force and is sometimes described as “shear modulus”.

- 1 GPa = 0.145x106 psi (lbf/in2)

- 1 x 106 psi = 6.9 GPa

### Here are examples of common materials:

| Material | Shear Modulus |  |
| --- | --- | --- |
|  | (106 psi) | (GPa) |
| Aluminum Alloys | 3.9 | 27 |
| Aluminum, 6061-T6 | 3.8 | 24 |
| Aluminum, 2024-T4 | 4.0 | 28 |
| Beryllium Copper | 6.9 | 48 |
| Brass | 5.8 | 40 |
| Bronze | 6.5 | 44.8 |
| Cadmium |  | 19 |
| Carbon Steel | 11.2 | 77 |
| Cast Iron | 5.9 | 41 |
| Chromium |  | 115 |
| Concrete | 3.0 | 21 |
| Copper | 6.5 | 45 |
| Glass, 96% silica | 2.8 | 19 |
| Inconel | 11.5 | 79 |
| Iron, Ductile | 9.1 - 9.6 | 63 - 66 |
| Iron, Malleable | 9.3 | 64 |
| Kevlar | 2.8 | 19 |
| Lead | 1.9 | 13.1 |
| Magnesium | 2.4 | 16.5 |
| Molybdenum | 17.1 | 118 |
| Monel metal | 9.6 | 66 |
| Nickel Silver | 6.9 | 48 |
| Nickel Steel | 11.0 | 76 |
| Nylon | 0.59 | 4.1 |
| Phosphor Bronze | 5.9 | 41 |
| Plywood | 0.09 | 0.62 |
| Polycarbonate | 0.33 | 2.3 |
| Structural Steel | 11.5 | 79.3 |
| Stainless Steel | 11.2 | 77.2 |
| Steel, Cast | 11.3 | 78 |
| Steel, Cold-rolled | 10.9 | 75 |
| Tin |  | 18 |
| Titanium, Grade 2 | 5.9 | 41 |
| Titanium, Grade 5 | 5.9 | 41 |
| Titanium, 10% Vanadium | 6.1 | 42 |
| Tungsten |  | 161 |
| Wood, Douglas Fir | 1.9 | 13 |
| Zinc |  | 43 |
| Z-nickel | 11 | 76 |

Please only use the Gpa (metric) units in coursework but be aware that colleagues will use both in real life...